## Slide 1: Ceramics
Apiwat Muttamara

## Slide 2: Topic
Traditional and Engineering ceramics
Simple ceramic crystal structures
Processing of ceramics
Properties of ceramics
Glasses

## Slide 4
Clay Products:
Structural products (Bricks, tiles, sewer pipes)
Whitewares (Porcelain, pottery, tableware, china, plumbing fixtures)
These products are composed of:
Alumina (Al2O3) + Silica (SiO2)

## Slide 5
Ceramics are compounds between metallic and nonmetallic elements
which can be oxides, nitrides, and carbides.
The wide range of materials that falls within this classification includes ceramics that are composed of clay minerals, cement and glass.
Products that are considered to be traditional ceramics are china, porcelain, bricks, tiles and in addition, glasses and high-temperature ceramics.
Notes: Since the atomic bonding in ceramic materials is either partially or totally ionic, most ceramic crystal structures may be thought of as being composed of electrically charged ions instead of atoms. The metallic ions are positively charged cations and the nonmetallic ions are negatively charged anions. Ceramics are composed of at least two elements and their crystal structures are far more complex than those of metals
Since the atomic bonding in ceramic materials is either partially or totally ionic, most ceramic crystal structures may be thought of as being composed of electrically charged ions instead of atoms. The metallic ions are positively charged cations and the nonmetallic ions are negatively charged anions. Ceramics are composed of at least two elements and their crystal structures are far more complex than those of metals
Over the years, significant progress has been made in understanding the fundamental character of ceramics and of the phenomena that occur in them that are responsible for their unique properties. Consequently, a new generation of these materials has evolved, and the term “ceramic” has taken on much broader meaning. These new materials have a rather dramatic effect on our lives; electronics, computer, communication, aerospace and a host of other industries rely on their use.

## Slide 6: Comparison
Ceramics
Metals

## Slide 7: electroluminescence
R C insulating Mat

## Slide 8
Boron nitride
Corelle

## Slide 9: Ceramics
1.Traditional ceramics ‑
clay products such as
pottery and bricks,
common abrasives, and cement
2.New ceramics ‑ more recently developed ceramics based on oxides, carbides, etc., and generally possessing mechanical or physical properties superior or unique compared to traditional ceramics

## Slide 10
(Classification based on application)

## Slide 11
Properties of Ceramic Materials
Crystalline and noncrystalline states
High melting temperatures (varying from 3500 to 7000 o F)
All ceramics are brittle at room temperatures
Very low resistance to tensile loads. Very low fracture strengths. Microcracks are formed very easily under tensile stresses.
Stronger under compressive loads and microcracks are not formed as easily as in tension.

## Slide 12
Properties of Ceramic Materials (Cont’d)
High hardness nd good wear resistance.
High toughness
Low thermal and electrical conductivity.
High creep resistance at elevated temperatures
Capacity to remain unreactive and inert when exposed to severe environments
Can be magnetized and demagnetized, some can be permanently magnetized

## Slide 13: Advanced Ceramics
Structural: Wear parts, bioceramics, cutting tools, engine components, armour.
Electrical: Capacitors, insulators, integrated circuit packages, piezoelectrics, magnets and superconductors
Coatings: Engine components, cutting tools, and industrial wear parts
Chemical and environmental: Filters, membranes, catalysts, and catalyst supports

## Slide 14: Engine Components
Rotor (Alumina)
Gears (Alumina)

## Slide 15: Ceramic Brake Discs

## Slide 16: Silicon Carbide
Automotive Components in Silicon Carbide
Chosen for its heat and wear resistance

## Slide 17
Piezoelectric
Quatz
Piezzein+electric
สนามไฟฟ้า
Notes: พวกนี้จะใช้พลังงานไฟฟ้าบางส่วนส่งผ่านผลึกควอทซ์ แล้วรับสัญญาณความถี่ กลับออกมาให้ ไมโครโพเซสเซอร์ประเมินออกมาเป็นเวลา

## Slide 18
Unit Cell at Rest
Neutral Charge
Unit Cell Under Mechanical
Compression (“pushing” force):
Electrical polarity as shown
Unit Cell Under mechanical
Tension (“pulling” force):
Electrical polarity reverses.
+ + +
-
+
+
-
+
-
- - -
-
+
+
-
+
-
+ + +
- - -
+
piezoelectric

## Slide 19
Crystals Quartz SiO2 Berlinite AlPO4 Gallium orthophosphate GaPO4 Tourmaline Ceramics Barium titanate BaTiO3 Lead zirconate titanate PZT
Other materials Zinc oxide ZnO Aluminum nitride AlN Polyvinylidene fluoride PVDF More piezo materials
Raincap

## Slide 20
Zirconia (ZrO2)
Properties:
the highest strength and toughness at room temperature
excellent surface smoothness
Applications:
household appliances and pump parts
Household appliances

## Slide 21: Al2O3
Heaters
Vacuum circuit breaker
Ceramic centrifugal pump
Liners of sliding surfaces for carrying and storing powder, Valves for chemical analysis, Rollers, nozzles, seal valves,
and grinding machine parts

## Slide 22: Bioceramics

## Slide 23
Non-oxide ceramics: SiC, Si3N4, BN, TiN
  Heat-resistance and high temperature structural material
  Corrosion and wear resistance
Drilling tool
Cutting tool

## Slide 24: Blade material and major uses
Carbon steel, steel alloy | Slow cutting
High-speed steel | General cutting, difficult-to-cut material
Coated super-hard alloys | General cutting
Ceramics | High-speed cutting finishing cuts
Sintered Diamond | Non-ferrous alloy, non-metal material cutting
Sintered cubic boron nitride (CBN) | Super-hard alloy, quenched steel, finish cut

## Slide 25
Silicon carbide (SiC)
Properties:
high temperature strength
highest corrosion resistance
Applications:
mechanical seals and pump parts
Silicon nitride (Si3N4)
Properties:
Heat resistance,
High temperature strength
Applications:
Engine and gas turbine parts

## Slide 26: Hardness of Ceramics

## Slide 27: Relative Hardness
B4C, SiC
WC, Al2O3
Glass

## Slide 28: Ceramic Phase Diagrams: Al2O3-Cr2O3 System
Notes: Note: They are similar to metal alloy systems - except the temperatures are generally higher.

## Slide 29
Stress-strain behavior for aluminum oxide and glass

## Slide 30: High purity alumina
manufacturing of sapphire for cover glass,
single crystal, translucent alumina ceramics
transparent alumina
sheaths for high-voltage sodium lamps

## Slide 31: Processing of Ceramics

## Slide 32
Pressing-(Plastic forming)
(Casting)
milling: Particle Size Distribution
Raw materials : Chemicals & minerals
powder
Green body
Ceramic product
(heat) :Sintered
Ceramics’Production processes

## Slide 33: Ceramics forming

## Slide 35: Thermal Treatment
Drying process or de-binding
  Debinder- organic binder ~ 200-300oC
  Green ware

## Slide 36
Sintering
  solid-state diffusion
  porous compact
  Temp. less than melting Temp.
  Ex. Al2O3 spark plug is sintered at 1600oC (melting point Al2O3 is 2050oC)

## Slide 37
Uniaxial pressing
  -Economic
    Mass production
    Tile, Electronics’industry
Powder Pressing

## Slide 38
  Isostatic Pressing
    Rubber Mold
    High Quality, Intricate parts
    Spark plug

## Slide 39
  Hot pressing
    Uniaxial pressing OR HIP
      reduce the porosity of metals. This improves the mechanical properties and increases workability.
    Mold mist be good thermal shock resistance
    Si3N4 , SiC, Al2O3

## Slide 40: Extrude
Cordiarite ceramics ( 2MgO.2Al2O3.5SiO2 )
Honey comb for gas purification catalyst carriers

## Slide 41: Amorphous Ceramics (Glasses)
Insulator
Chemical resistance
Good corrosion resistance
Main ingredient is Silica (SiO2)
If cooled very slowly will form crystalline structure.
If cooled more quickly will form amorphous structure consisting of disordered and linked chains of Silicon and Oxygen atoms.
This accounts for its transparency as it is the crystal boundaries that scatter the light, causing reflection.
Glass can be tempered to increase its toughness and resistance to cracking.

## Slide 42: Glass Types
Three common types of glass:
Soda-lime glass - 95% of all glass, windows containers etc.
Lead glass - contains lead oxide to improve refractive index
Borosilicate - contains Boron oxide, known as Pyrex.

## Slide 43: Glasses
Flat glass (windows)
Container glass (bottles)
Pressed and blown glass (dinnerware)
Glass fibres (home insulation)
Advanced/specialty glass (optical fibres)

## Slide 44: Silicate glasses
Amorphous silica forms a “network” with relatively large open areas where foreign atoms and particles may be easily introduced.
Silicates: amorphous silica with impurities
Sodium-silicate glass
Glass-modifying oxide
Ex. Na2O, K2O, CaO , MgO
(reduce viscosity)
  Intermediate oxides
  Improve properties
  Ex.Al2O3 Improve melting point

## Slide 45
  Vitrification is a process
  of converting a material
  into a glass-like amorphous solid which is free of any crystalline structure, either by the quick removal or addition of heat, or by mixing with an additive. Solidification of a vitreous solid occurs at the glass transition temperature (which is lower than melting temperature, Tm, due to supercooling).
Vitrification

## Slide 46: Glass Transition
Tm : melting temperature
Tg : glass transition temperature
Temp. < Tg  glass
Temp. > Tg  supercooled liquid

## Slide 48
Effect of Temp&Viscosity
The melting point (100 Poises) :
The working point (104 P):
The softening point (4 x 107 P): Without shape change
The annealing point (1013 P) :
  (residual stress)
The strain point ( 3x1014 P)

## Slide 49: Glass Forming
  pressing
  blowing
  drawing
  fiber forming

## Slide 50
Fiber forming

## Slide 51: Plate Glass Drawing Processes

## Slide 52: Tempered Glass
softening point rapid air cooling, oil bath
safety glass for door

## Slide 53: Chemically Strengthened Glass
Cations with large ionic radius are diffused into the surface
This strains the “lattice” inducing compressive strains and stresses.
Sodium aluminosilicate + Potassium nitrate at 50oC below strain point (500oC ) for 6-10 hours cause compressive stress นon Surface and tensile stress in the part.
Airplane glass , Optical glasses
Si4+
K3+
Na+
Al3+
Notes: Sodium aluminosilicate จุ่มใน Potassium nitrate ที่ 50oC ต่ำกว่า strain point (500oC ) เป็นเวลา 6-10 ชั่วโมง Potassium ions ซึ่งมีขนาดใหญ่กว่า Sodium ions จะไปแทนที่ Sodium ions ทำให้เกิด compressive stress ที่ผิว และ tensile stress ภายในชิ้นงาน
ใช้ทำกระจกสำหรับเครื่องบิน และเลนส์แว่นตา

## Slide 54: Structured like a single crystal
Polycrystal  not transparent
  grain boundaries or pore absorb or scatter light
Like a single crystal  transparent
  extra-high purity ceramics
  grains are sintered so close to each other
Application: protective goggles, camera shutters
Ordinary ceramics
Transparent ceramics

## Slide 55: Ceramic single crystal
MgO single crystal
Yttrium Aluminum Garnet (YAG) single crystal