## Slide 1
Die Design
Dr. Apiwat Muttamara

## Slide 2: Agenda
Material selection
Die Design
    Structure of Die

## Slide 3: Standards Designation Equivalent of Tool Steels ---
AISI | American Iron & Steel Institute
JIS | Japanese Industrial Standards
DIN | Deutsches Institut für Normung
 | (German Standards Institute)
SS | Svensk Standard
 | (Swedish Standard)
BS | British Standards

## Slide 5
 | DAIDO BRAND | JIS | AISI | DIN | 
Cold Work Tool Steels | YK30 | SKS93 | - | - | -
 | YK4 | SK4 | W1/W2 | 1.154 | C100W1
 | G0A | SKS3mod. | - | - | -
 | G05 | - | - | - | -
 | DC11 | SKD11 | D2 | 1.2379 | X165CrMoV12
 | DC53 | SKD11mod. | - | - | -
Hot Work Tool Steels | DHA1 | SKD61 | H13 | 1.2344 | X40CrMoV51
 | DH2F | SKD61mod. | - | - | -
 | GFA | SKT4mod. | L6 | 1.2714 | 55CrNiMoV6

## Slide 6
 | DAIDO BRAND | JIS | AISI | DIN | 
High Speed Tool Steels | MH51 | SKH51 | M2 | 1.3343 | S6-5-2
 | MH85 | - | - | - | -
Plastic Mold Steels | PXZ | - | - | - | -
 | PX4 | - | p20mod. | - | -
 | PX5 | - | p20mod. | - | -
 | NAK55 | - | - | - | -
 | NAK80 | - | - | - | -
 | S-STAR | SUS420J2mod. | 420mod. | 1.4034 | X40Cr13
 | G-STAR | - | - | - | -

## Slide 7
Application | Usual Hardness HRC | Recommended DAIDO BRAND | 
 |  | General Uses | 
 |  | Short Life | Long Life
Trimming Dies | 58-62 | YK30 | GOA
Pressing Dies | 58-63 | YK30 | GOA
Crimping Dies | 58-63 | GOA | DC11
Extrusion Dies | 55-62 | GOA | DC11
Extrusion Punches | 55-62 | GOA | DC11
Brick Forming Dies | 60-65 | GOA | DC11
Powder Compacting Dies | 58-62 | GOA | DC11
Cross Punches | 60-64 | MH51 | MH51
Plastic Mold Dies | 56-60 | GOA | -

## Slide 8
Back post
Die set

## Slide 11
Steel | I=1.5D
Cast Iron | I=2D
Aluminum | I=2.5D
Plastic | I=3D up
H > 1.5D | 
J = I+3 | K=3
O > D | 
P > D | 

## Slide 12: Guide & Bush

## Slide 16
8

## Slide 21: Stopper

## Slide 22: Front space

## Slide 23: Stripper plate
Pin

## Slide 24: Relief Angle

## Slide 26
Location of bolts

## Slide 27: Punch Plate

## Slide 28: Stripper Thickness