## Slide 1
Welding
Notes: Text book,
Office hour, by appointment

## Slide 2: Joining and Assembly
Joining - welding, brazing, soldering, and adhesive bonding
These processes form a permanent joint between parts
Assembly - mechanical methods (usually) of fastening parts together
Some of these methods allow for easy disassembly, while others do not

## Slide 3: Types of Welding Processes
Welding processes can be divided into two major categories:
Fusion welding
  Arc welding (AW)
  Resistance welding (RW)
  Oxyfuel gas welding (OFW)
Solid state welding: Joining processes using pressure alone or a combination of heat and pressure
  If heat is used, temperature is below melting point of metals being welded
  No filler metal is added in solid state welding

## Slide 4: Types of Welding
Fusion Welding
Pressure Welding
Homogeneous
Heterogeneous
Brazing
Soldering
Gas Welding
Electroslag
High Energy Beam
Electric Arc
MIG
TIG
Shielded Metal Arc – “Stick”
Friction Welding

## Slide 5: Five Types of Joints
(a) Butt joint, (b) corner joint, (c) lap joint, (d) tee joint, and (e) edge joint

## Slide 6
(a) Square groove weld, one side; (b) single bevel groove weld; (c) single V‑groove weld; (d) single U‑groove weld; (e) single J‑groove weld; (f) double V‑groove weld for thicker sections (dashed lines show original part edges)
Groove Welds

## Slide 7
(a) Inside single fillet corner joint; (b) outside single fillet corner joint; (c) double fillet lap joint; (d) double fillet tee joint (dashed lines show the original part edges)
Fillet Welds

## Slide 8: Plug Weld and Slot Weld
(a) Plug weld and (b) slot weld

## Slide 9
Fused section between surfaces of two sheets or plates: (a) spot weld and (b) seam weld
Used for lap joints
Closely associated with resistance welding
Spot Weld and Seam Weld

## Slide 10
Typical Fusion Welded Joint

## Slide 11
A pool of molten metal is formed near electrode tip, and as electrode is moved along joint, molten weld pool solidifies in its wake
Arc Welding: The most common fusion welding
http://www.youtube.com/watch?v=TeBX6cKKHWY

## Slide 12: Two Basic Types of Arc Welding Electrodes
Consumable – consumed during welding process
  Source of filler metal in arc welding
Nonconsumable – not consumed during welding process (e.g. Tungsten)
  Filler metal must be added separately if it is added

## Slide 13: Arc Shielding
At high temperatures in arc welding, metals are chemically reactive to O2, N2 and H2 in air
  Mechanical properties of joint can be degraded by these reactions
  To protect operation, arc must be shielded from surrounding air in AW processes
Arc shielding is accomplished by:
  Shielding gases, e.g., argon, helium, CO2
  Flux

## Slide 14: Flux
A substance that prevents formation of oxides and other contaminants in welding, or dissolves them and facilitates removal
Provides protective atmosphere for welding
Stabilizes arc
Reduces spattering
Flux Application
Pouring granular flux onto welding operation
Stick electrode coated with flux material that melts during welding to cover operation
Tubular electrodes in which flux is contained in the core and released as electrode is consumed

## Slide 15: Consumable Electrode Arc Welding Processes
Shielded Metal Arc Welding
Gas Metal Arc Welding
Flux‑Cored Arc Welding
Electrogas Welding
Submerged Arc Welding

## Slide 16: Shielded Metal Arc Welding (SMAW)
Uses a consumable electrode consisting of a filler metal rod coated with chemicals that provide flux and shielding

## Slide 17: Welding Stick in SMAW
Composition of filler metal usually close to base metal
Coating: powdered cellulose mixed with oxides and carbonates, and held together by a silicate binder
Disadvantages of stick welding:
  Sticks must be periodically changed
  High current levels may melt coating prematurely

## Slide 18: SMAW Applications
Used for steels, stainless steels, cast irons, and certain nonferrous alloys
Not used or rarely used for aluminum and its alloys, copper alloys, and titanium

## Slide 19
Gas Metal Arc Welding
Uses a consumable bare metal wire as electrode with shielding by flooding arc with a gas
http://www.youtube.com/watch?v=wPeHA9Szhhg

## Slide 20: Inert Gas Welding
For materials such as Al or Ti which quickly form oxide layers, a method to place an inert atmosphere around the weld puddle had to be developed

## Slide 21: Metal Inert Gas (MIG)
Uses a consumable electrode (filler wire made of the base metal)
Inert gas is typically Argon
Inert gas is CO2 Called GMAW
BASE METAL
PUDDLE
POWER SOURCE
DRIVE WHEELS
CONSUMABLE ELECTRODE
ARC COLUMN
SHIELDING GAS

## Slide 22: GMAW Advantages over SMAW
Better arc time because of continuous wire electrode
  Sticks must be periodically changed in SMAW
Better use of electrode filler metal than SMAW
  End of stick cannot be used in SMAW
Higher deposition rates
Eliminates problem of slag removal
Can be readily automated

## Slide 23: Tungsten Inert Gas (TIG)
Tungsten electrode acts as a cathode
A plasma is produced between the tungsten cathode and the base metal which heats the base metal to its melting point
Filler metal can be added to the weld pool
Can be called (GTAW)
BASE METAL
PUDDLE
POWER SOURCE
SHIELDING GAS
TUNGSTEN ELECTRODE
Filler wire

## Slide 24
Presence or absence of externally supplied shielding gas distinguishes: (1) self‑shielded - core provides ingredients for shielding, (2) gas‑shielded - uses external shielding gases
Flux-Cored Arc Welding
http://www.youtube.com/watch?v=kI7GOVrB33c

## Slide 25: Oxyacetylene Welding
Flame formed by burning a mix of acetylene (C2H2) and oxygen
Fusion of metal is achieved by passing the inner cone of the flame over the metal
Oxyacetylene can also be used for cutting metals
Inner Cone: 5000-6300 deg F
Combustion Envelope 3800 deg F
2300 deg F
TORCH TIP

## Slide 26: Resistance Welding
Resistance welding, showing components in spot welding, the main process in the RW group
http://www.youtube.com/watch?v=66-RK0DPXfU

## Slide 27
Resistance Seam Welding
https://www.youtube.com/watch?v=xZ5SMBoIh4s

## Slide 28
Roll Welding

## Slide 29
(1) Rotating part, no contact; (2) parts brought into contact to generate friction heat; (3) rotation stopped and axial pressure applied; and (4) weld created
Friction Welding
http://www.youtube.com/watch?v=5JbnDXw-0pM 1 min

## Slide 30: Friction Stir Welding
(1) Rotating tool just before entering work, and (2) partially completed weld seam
http://www.youtube.com/watch?v=_qAOKR6mdTI 1.5 min

## Slide 31: Residual Stresses and Distortion
(a) Butt welding two plates
(b) Shrinkage
(c) Residual stress patterns
(d) Likely warping of weldment

## Slide 32: Techniques to Minimize Warpage
Welding fixtures to physically restrain parts
Heat sinks to rapidly remove heat
Tack welding at multiple points along joint to create a rigid structure prior to seam welding
Preheating base parts
Stress relief heat treatment of welded assembly

## Slide 33: Brazing
Joining process in which a filler metal is melted and distributed by capillary action between faying surfaces of metal parts being joined
No melting of base metals occurs
  Only the filler melts
Filler metal Tm is greater than 450C (840F)
  But less than Tm of base metal(s) to be joined
http://www.youtube.com/watch?v=m678-clpbjw 3 min

## Slide 34: Brazing Compared to Welding
Any metals can be joined, including dissimilar metals
Can be performed quickly and consistently, permitting high production rates
Multiple joints can be brazed simultaneously
Less heat and power required than Fussion Welding
Problems with HAZ in base metal are reduced
Joint areas that are inaccessible by many welding processes can be brazed
  Capillary action draws molten filler metal into joint

## Slide 35: Disadvantages and Limitations of Brazing
Joint strength is generally less than a welded joint
Joint strength is likely to be less than the strength of the base metals
High service temperatures may weaken a brazed joint
Color of brazing metal may not match color of base metal parts

## Slide 36: Brazing Applications
Automotive (e.g., joining tubes and pipes)
Electrical equipment (e.g., joining wires and cables)
Cutting tools (e.g., brazing cemented carbide inserts to shanks)
Jewelry
Chemical process industry
Plumbing and heating contractors join metal pipes and tubes by brazing
Repair and maintenance work

## Slide 37: Soldering
Joining process in which a filler metal with Tm less than or equal to 450C (840F) is melted and distributed by capillary action between faying surfaces of metal parts being joined
No melting of base metals, but filler metal wets and combines with base metal to form metallurgical bond
Filler metal called solder
Closely associated with electrical assembly
http://www.youtube.com/watch?v=BLfXXRfRIzY

## Slide 38: Soldering Advantages and Disadvantages
Advantages:
Lower energy than brazing or fusion welding
Variety of heating methods available
Good electrical and thermal conductivity in joint
Easy repair and rework
Disadvantages:
Low joint strength unless reinforced mechanically
Joint weakens or melts at elevated temperatures

## Slide 39: Solders
Traditionally alloys of tin and lead (both have low Tm)
Lead is poisonous and its percentage is minimized in most solders
Tin is chemically active at soldering temperatures and promotes wetting action for successful joining
  In soldering copper, copper and tin form intermetallic compounds that strengthen bond
Silver and antimony also used in soldering alloys

## Slide 40: Soldering Methods
Many soldering methods are same as for brazing, except less heat and lower temperatures are required
Additional methods:
  Hand soldering – manually operated soldering gun